	ЭП866 - 15Х16К5Н2МВФАБ; ВНС-30 

Сталь 15Х16К5Н2МВФАБ применяется: для изготовления фасонного проката и поковок, предназначенных для последующей холодной механической обработки, либо для последующей горячей механической обработки (штамповки, ковки, прокатки и т. п.) при изготовлении деталей машин и деталей специальной техники.

Коррозионностойкая жаропрочная сталь мартенситного класса.

ЭП609 - 07Х12НМБФ, 

Сталь 07Х12НМБФ применяется: для изготовления листового и фасонного проката, прутков горячекатаных и кованых, а также поковок, предназначенных для последующей холодной механической обработки, либо для последующей горячей механической обработки (штамповки, ковки, прокатки и т. п.) при изготовлении деталей машин; колец цельнокатаных различного назначения; сварочной проволоки. 

40ХН2МА
Сталь 40ХН2МА применяется: для изготовления цельнокатаных колец, коленчатых валов, клапанов, шатунов, крышек шатунов, ответственных болтов и других крепежных деталей, специального крепежа, шестерней, кулачковых муфт, дисков и других тяжелонагруженных деталей; для производства валков для холодной прокатки металлов; для изготовления деталей трубопроводной арматуры; деталей авиастроения (валов ротора, коленчатых валов, валов редуктора, шатунов двигателя воздушного охлаждения, ответственных болтов, шпилек, деталей винта, массивных и силовых деталей РД), работающих при температуре до +500°.

Сталь конструкционная высококачественная хромоникельмолибденовая.

Сталь 40ХНМА по сравнению со сталью 18ХНВА менее легирована, но содержит больше углерода и нечувствительна к отпускной хрупкости.

	EP866 - 15KH16K5N2MVFAB; VNS30 

Steel 15Х16К5Н2МВФАБ is used in applications as follows: manufacturing shaped bars and forgings designed for a subsequent cold machining or for a subsequent hot machining (stamping, forging, rolling, etc.); manufacturing machine parts and special equipment parts.

Corrosion-resistant martensitic heat-resistant steel type.

EP609 - 07Х12НМBF 

Steel 07Ch12NMBF is used in applications as follows: manufacturing sheet and shaped rolled products, hot-rolled and forged bars, as well as forged parts intended for a subsequent cold machining, or for a subsequent hot machining (stamping, forging, rolling, etc.); manufacturing machine parts; rolled rings for various purposes; welding wire. 

40XN2MA
Steel 40XN2MA is used in applications as follows: manufacturing solid rolled rings, crankshafts, valves, connecting rods, connecting rod caps, critical bolts and other fasteners, special fasteners, gears, cam couplings, disks and other heavy-duty parts; producing rolls for cold-rolling metals; manufacturing parts of pipeline fixtures; parts of aircraft construction (rotor shafts, crankshafts, gear shafts, connecting rods of air cooling engine, critical bolts, studs, propeller parts, massive and power parts of working engine), working at temperatures up to +500 °.

High-quality chromium-nickel-molybdenum structural steel.

Steel 40XNMA is less alloyed than steel 18XNVA, but contains more carbon and is insensitive to temper embrittlement.
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