Radial thickeners
Radial thickener with central drive (C) is intended for thickening and pulp deslurring, 

white water, solution and suspension clarification and purification in  ore-mining plants, in metallurgical, coal, chemical and other industries.
On customer’s request it is possible to design and produce thickeners in acid-resisting construction

	Parameters

Tank diameter,m

Tank depth in the center,m
Thickening area, m²
Duration of 1 revolution of revolving arms, min
Rated unit load (capacity) of the thickened product, t/m² d*
Capacity of the electric motor of revolving arms drive, kW
Height of revolving arms hoisting, mm

Mass, kg


	C25M

25

5,0

490

12…23

6

2x1,6
500

52000
	C30M

30

5,4

700

12…23

6

2x2

500

55400
	C50M

50

6,1

1950

17; 26; 38

4

2x7,5

-

66000
	C100M

100

8,5

7850

33…80

4

4x2,5

-

214000


Climatic service                                              in the open area at the temperature

conditions                                    up to -40˚C                                            up to -55˚C

*Actual thickener capacity of the thickened product, depending on different technology factors, that is: on pulp and hard fraction characteristics, type, quantity, the condition of the flocculant supply, power and discharge mode etc., is defined and revised taking into consideration actual operating conditions. 
[image: image1.png]



Radial thickener C50M
Deep radial thickeners with weighed layer     
Are intended for thickening and pulp, solution and suspension deslurring, also including fine and hard precipitated fraction, as well as for waste and white water clarification. May be used in coal preparation plants, mining-and-processing integrated works, in metallurgical, chemical and others productions.             

On customer’s request it is possible to design and produce thickeners in acid-resisting construction

	Parameters 

Tank diameter, m

Tank depth in the center,m

Thickening area, m²

Duration of 1 revolution of revolving arms, min

Maximum rated unit load (capacity) of the thickened product, permitted by the thickener’s construction t/m² d*

Capacity of the electric motor of revolving arms drive, kW

Height of revolving arms hoisting, mm

Feed rate at the concentration by weight in the feed 30…50 g\l, m³/hr
Concentration by weight in the thickened product no less than, kg/ m³**
Mass, kg, including tank
	DTW-18

18
12,0

250

13…20

5

2x2

400

Up to 1200

500
172100

106500 (metallic)
	DTW-25

25
11,7

490

13…20

5

1,6x2

400

Up to 2500

500

67600

(reinforced concrete)


	DTW-30

30
11,7

700

13…20

5

1,9x2

400

Up to 3200

500

72200
(reinforced concrete)


*Actual thickener capacity of the thickened product, depending on different technology factors, that is: on pulp and hard fraction characteristics, type, quantity, the condition of the flocculant supply, power and discharge mode etc., is defined and revised taking into consideration actual operating conditions. 


** The indexes refer to the finely dispersed suspensions thickening, slurry coal and flotation tailings left after the coal benefication in particular. 

Radial thickener, closed type

G-40 Thickener is intended for suspension and solution thickening and washing at high temperature, particularly, “red mud” in alumina production. May be used in non-ferrous metallurgy plants, specifically in alumina industry while nickel and cobalt production. 
	Tank diameter, m

Tank height at the periphery, m 

Thickening area, m²

Height of revolving arms hoisting, mm

Period of rotation of revolving arms, min

Throughput of feeding pulp, no less, m³/hr

Solid phase content in clarified solution, g/l

Drive energy input, kw

Rake suspension

Revolving arms metal ware cleaning device

Cleaning period (no less), months*

Mass, kg
	40,0
6,0

1250

500

10; 15; 20

425

0,15

6,5

Flexible ropes

Vibratory, of cyclic automatic operation

12

60000



*in alumina production
